CHEM 351   		Principles of Organic Chemistry II Laboratory		Prof. Nalli

Summer 2014										WSU

Experiment #7. Organic Dyes

# Overview

The process of dyeing is one of the earliest types of chemical process used by humans. The overall process involves both a colored compound (a pigment) and a mechanism for pigment adhesion to the fabric. In this lab you will dye various fabrics via two common adhesion mechanisms: physical entrapment and covalent bonding. Physical entrapment refers to cases where the dye is induced to form solid particles within the fabric which become entrapped within the network of fibers. Two examples that use physical entrapment are indigo vat dyeing and diazo development dyeing. Covalent bonding is the mechanism used by the so called “fiber reactive” dyes used to form the brilliant color-fast colors seen in many modern garments.

Part 1. Diazo Development Dyeing. Arenediazonium salts (ArN2+Y) are useful for the synthesis of compounds, such as iodoarenes (ArI),  because they enable nucleophilic aromatic substitution  by nucleophiles for the diazonio group (N2+), which is a super leaving group (eq 1). However, the outer nitrogen atom of the diazonium salt is also an electrophilic site and can serve as the electrophilic atom in aromatic substitution reactions on activated benzene rings (eq 2). The products of equation 2 are highly colored and referred to as azo dyes.

+

Ar-NN:     +    I:                                              Ar-I     +     :NN:     (1)

+

Ar-NN:     +    Ar’H                                              Ar-N=N-Ar’     (2)

The diazonium salt can be prepared using sodium nitrite and hydrochloric  acid from the corresponding aromatic amine in a process termed "diazotization" (eq 2).

Ar-NH2   +    NaNO2   +  2 HCl                              ArN2+Cl    +   2 H2O  +  NaCl      (3)

In this part of the experiment you will carry out the diazotization of p-nitroaniline. Then a cloth which has been soaked in basic 2-naphthol solution will be immersed in the diazonium solution forming an insoluble bright red azo dye within the fiber network of the cloth.

# Procedure for Diazo Dyeing

Dissolve 3.0 mL HCl(conc) in 10 mL H2O in an Erlenmeyer flask. Swirl the solution while adding 100 mg p-nitroaniline. Chill the mixture on an ice bath. Prepare a solution of 100 mg NaNO2 in 5 mL H2O. After the temperature of the p-nitroaniline/HCl solution has reached about 5C begin a slow addition of the NaNO2 solution. (Use a Pasteur pipet to add the solution one drop at a time.) The rate of addition should be slow enough so that the temperature of the reaction mixture never exceeds 10C. (Above this temperature the diazonium salt undergoes nucleophilic substitution by H2O resulting in phenol formation.) Keep the solution on ice until use in the next part.

Soak a piece of fabric (note the type of fabric used) in a solution of 100 mg 2-naphthol dissolved in 5 mL 5% NaOH(aq). Remove the cloth, squeeze it to remove most of the solution, and then immerse it in the cold diazonium solution. The insoluble azo dye will form within the fabric. Allow the reaction to proceed for 5-10 min then remove the fabric and rinse it in cold water and set it on paper towels to dry.

Waste beakers for the left over diazonium  and 2-napthol solutions will be available in the dispensing hood.

Part 2. Indigo Vat Dyeing.

In this process the deeply colored, insoluble indigo is reduced to a soluble, colorless form by sodium dithionite (Na2S2O4) (eq 4). The fabric is immersed in the colorless solution of reduced dye and then removed. Upon removal, the indigo air-oxidizes back to the insoluble form leaving blue particles trapped within the fibers.

(4)

# Procedure for Indigo Vat Dyeing

Prepare a solution of 1.5 g NaOH(s) in 5 mL water in a 50-mL Erlenmeyer flask. Add 1.5 g indigo and a magnetic stir bar to the solution. Add 20 mL water to the stirring mixture. Heat the solution to approx 50 °C and then add 5.0 g of Na2S2O4 in small portions. Keep stirring the solution at approx 50 °C (use a hot water bath) for 20-30 min. At this point the solution should be light yellow with no sign of undissolved indigo powder. Add this solution to 300 mL of warm (approx. 50 °C) water a large beaker. (If a blue or greenish tint develops then add a few mg of additional dithionite.) Use this solution to dye a cotton bandana. Repeated immersions will work best to develop a darker color. Hang the bandana up to dry in the back of the fume hood.

Part 3. Tie-dyeing with Fiber-Reactive Dyes.

Fiber-reactive dyes adhere to cotton (essentially cellulose) through the formation of ether linkages to the OH groups of the cellulose. They consist of a colored moiety (often an azo dye) linked to a dichlorotriazene group (Scheme 1). The cellulose is activated by treatment with base (Na2CO3) to form alkoxide groups which then undergo nucleophilic attack on the triazene rings and substitute for the chlorine leaving groups (Scheme 2). Both chlorines can be replaced and to the extent that this occurs the fibers of the fabric will be cross-linked, thus enhancing its durability.

Procedure for Tie Dyeing

See http://www.prochemical.com/directions/MX%20PDF/Tie%20Dye.pdf. Most of steps 1-3 have been done for you.

Soak the t-shirt in soak solution (aqueous Na2CO3) for at least 10 min and then ring it out as described in step 2 before tying up and applying dye.

Make a dye solution to share with the rest of the class by dissolving one of the available Procion™ Dyes in 400 mL of 10% aqueous urea. See the table in step 4 of the above linked document for the approximate amount of dye powder to use.

Tie up the soaked t-shirt using rubber bands according to your creative desires. See http://www.prochemical.com/directions/Folding.htm for ideas.

Use a 50-mL plastic syringe to apply dye solutions to the t-shirt. See step 5 of the linked procedure.

Place the t-shirt in the supplied plastic bag and bring it home and allow the dye to cure for at least 4 hours but preferably overnight.

Rinse the garment as described in step 6 and then wash it (if using a washing machine do it in a load by itself) using ordinary laundry detergent.

Scheme 1. Fiber-Reactive Dyes and Cellulose Structures

Scheme 2. Reaction of Fiber-Reactive Dyes with Activated Cellulose and Water