## Slide 1: BONDED JOINTS

## Slide 2: BONDED/MECHANICAL JOINT COMPARISON
adhesion science - see Loctite, pgs 22 and 23
brainstorming exercise
  advantages of adhesive joints over mechanical joints
  advantages of mechanical joints over adhesive joints
compare with list from Strong, pg 167

## Slide 3: TAPE EXPERIMENT

## Slide 4: TYPES OF JOINTS
joint designs – see Loctite, pg 150 and 151

## Slide 5: JOINT SHOULD BE LOADED IN SHEAR NOT IN PEEL
shear stress distribution in adhesive (see Fig. 2, pg. 684, ASM Vol. 1)
tapering edges will help eliminate stress risers under loading - reducing tendency to peel (especially in lap joints)
influence of bonded lengths in flat lap joints (see Fig. 22.14, pg. 616, Lubin)
performance of different joint types (see Figs. 22.9 and 22.10, pg. 614, Lubin)

## Slide 6: CREEP
continued strain at constant load
dependent on
  joint configuration
  stress level
  type of adhesive
  orientation of adherends
generalized characteristics of creep (old reference)
  brittle adhesives exhibit less creep than do ductile adhesives
  a reduction of 30% in either stress or operating temperature level increases creep durability 500 times

## Slide 7: FATIGUE
symmetrical bonded joints have higher fatigue endurance limits than unsymmetrical bonded joints
generalized characteristics of fatigue resistance
  an increased depth of lap creates increased fatigue life
  adhesive fatigue life decreases slightly with increased thickness of adherends

## Slide 8: DESIGN OF BONDED JOINT
adhesive selection
  ability to withstand required stresses
  ability to withstand in-service environmental conditions
  practicality of the application process
    mode of surface preparation
    restriction on handling prepared surfaces before bonding
    method of mixing and applying adhesive to joint
    fixturing necessary for support of joint during bonding
    method of cleaning joint after bonding
  types of adhesive (see Table 1, pg. 684, ASM Vol. 1)
analysis of joint to determine area of bond

## Slide 9: BONDED JOINT PROCESS
dry fit and/or imprint
prepare surfaces
apply adhesive
  maintain thickness of bond (from Strong: 0.004 in. - 0.008 in., from Hercules: 0.005 in. - 0.015 in.)
  to maintain bondline thickness use bond wires, glass beads, or scrim cloth
place in a locating/bonding fixture
compact to remove entrapped air
clean up
cure

## Slide 10: PREPARATION OF COMPOSITE ADHEREND
surface must be free of grease and other contaminants (i.e. mold release agent)
  wipe with solvent or vapor degreasing
  rinse with water or alkaline solution (to remove solvents)
abrade surface with sandpaper (or Scotchbrite)
wipe again with solvent
rinse with water (dry in oven if rinsed with water)
peel ply may be used to eliminate sanding
water break test to ensure proper surface preparation

## Slide 11: PREPARATION OF METAL ADHEREND
aluminum - phosphoric acid anodizing (PAA) followed by primer
titanium - phosphate fluoride or some anodizing method
any metal which forms surface oxide should be carefully treated to achieve stable surface

## Slide 12: BONDING OF THERMOPLASTICS
materials can be welded (fusion bonded) rather than adhesively bonded
welding process
  conventional heating, ultrasonic heating, friction heating and induction heating (requires metal screen - susceptor)
  clean surfaces with solvent and/or water and detergent
  heat surfaces to point of incipient melting
  press surfaces together