## Slide 1: FINISHING OF COMPOSITES

## Slide 2: APPROACH TO FINISHING COMPOSITES
Composite materials can be trimmed and cut more easily with processes closer to grinding or abrasive cutting than conventional metal cutting which produces large chips
Cutting, machining and drilling processes dictated by reinforcement

## Slide 3: CONVENTIONAL METAL WORKING EQUIPMENT AND VARIOUS ABRASIVE MATERIALS HAVE BEEN USED WITH MINIMAL MODIFICATIONS
in most cases cutting speed (spindle speed) should be increased and the feed rate decreased relative to usual values for metal machining
cooling or lubricating fluid may be necessary (especially with thermoplastics) to prevent resin build-up on cutting tool and overheating of part
diamond or tungsten carbide tipped tools are recommended (must be kept sharp to minimize delaminations)
efficient vacuum system capable of removing cut material and dust will significantly increase cutter life

## Slide 4: BRITTLE NATURE OF COMPOSITES NEEDS TO BE REMEMBERED IN MACHINING OPERATIONS
holding fixtures should provide for backing of part to prevent delamination and back-side breakout
when milling, both edges should be cut and then center (rather than starting at one edge and working toward other edge), possibility of breaking off last edge section is minimized

## Slide 5: SANDING
bulk removal - 80 grit
finish sanding - 240 to 320 grit (wet)

## Slide 6: SAWING (BANDSAW)
fine offset
high-strength-steel stagger-tooth blade
reverse blade for cleaner cuts
good success with bandsaw blade with diamond grit on cutting edge and a relief cutout (area without grit) every 2-4 in.

## Slide 7: HISTORY OF DRILLING IN COMPOSITES
due to abrasive nature of fibers only tungsten carbide tooling (used on cast iron) can drill through it
properly designed cast iron cutting tip heats metal to provide plastic flow needed for efficient cutting
  neutral rake
  wide chisel point
  scrapes material causing resistance to penetration -> pressure must be exerted
composites cannot tolerate heat
pressure causes fibers to hinge resulting in furry, undersized hole as tool plunges through last few fibers

## Slide 8: DRILLING IN COMPOSITES
drill bits
  tungsten carbide or polycrystalline diamond
  large positive rake angle (see figure)
  chisel edge close to being a point
  high helix angles and polished flutes to accommodate chip lifting and removal
  resulting chips should appear as confectioners’ sugar
peck drilling of deep holes

## Slide 9: WORKING WITH ARAMID FIBER REINFORCED COMPOSITES
fibers tough and tend to shred not cut
fibers need to be preloaded (stretched) and then cut
DuPont reference

## Slide 10: WATER-JET CUTTING
utilizes fine, high-pressure jet to impact -> cuts or erodes material
intensifier pumps pressurize water to 60,000 psi
pumped at low volumes, 1 - 2 gals/min
through sapphire orifice (0.010 in. in dia.)
abrasives can be added (after primary jet is formed)
YouTube video

## Slide 11: ADVANTAGES OF WATER-JET CUTTING
can be initiated at any point on part (however usually started at edge or away from finished area - delamination can occur in area of initial penetration)
can cut complex patterns
can be numerically controlled
can dwell in one place for some time without widening cut width

## Slide 12: DISADVANTAGES OF WATER-JET CUTTING
noisy
filtration equipment for water
carefully monitor for jet wear
tendency to produce trailback especially in thicker materials (fig. 5 at www.wardjet.com)
exposing composite to water
cutting speed (in comparison to laser cutting)

## Slide 13: LASER CUTTING AND DRILLING
coherent beam of light focused onto workpiece and then burns or melts materials away
YouTube video

## Slide 14: ADVANTAGES OF LASER CUTTING AND DRILLING
no cutting force exerted (fragile pieces can be cut)
can be started at any point in workpiece
can cut complex patterns
can be focused or collimated with apertures to drill holes which are too small to be effectively drilled mechanically

## Slide 15: DISADVANTAGES OF LASER CUTTING AND DRILLING
thermal effects may be serious detriment
  melted or charred edge or heat-affected zone surrounding cut
  more severe for carbon fibers due to good heat conductivity property
difficult to cut thick parts (no way to remove waste material - interferes with beam)
need to be aware of resin systems that may produce hazardous fumes