## Slide 1: MECHANICAL JOINTS

## Slide 2: A MAJOR CONCERN WHEN MECHANICALLY JOINING COMPOSITES
(carbon reinforced) composites are more sensitive to high bearing loads than metals (design with as much bearing surface as is practical)

## Slide 3: LOADING OF LAP SHEAR SPECIMEN IN TENSION
eccentricity begins to develop and fastener tipping or "cocking" occurs (see fig. 1, pg. 707, ASM Vol. 1)
little change is noted by changing angle of head -> big difference is in area of bearing that supports the reaction load (130 degree flush head was developed) (see figs. 2 and 3)
Comp-Fast fasteners – prior to load, following load
as distance between centroids becomes greater reaction loads go up in value -> 130 degree head will not be satisfactory, limited to thin structures (see fig. 4)
the tension head optimizes head bearing area and is recommended for both tension and shear applications where countersink depth does not exceed 70% of top laminate (see fig. 5)
protruding head configurations not as sensitive to performance

## Slide 4: FIT BETWEEN FASTENER AND HOLE/WORKPIECE
clearance fit
net fit
interference fit

## Slide 5: CLEARANCE FIT HOLES
when clearance fit holes are used high clamp-up load appears to be beneficial for joint strength and fatigue life
clamping forces must be spread out over sufficient area -> compressive strength of resin system cannot be exceeded or the composite will be crushed
high clamp-up load delays slippage of composite laminates and cocking of fastener in joint (which contribute to high concentration of bearing stresses, see fig. 6, pg. 707, ASM Vol. 1)

## Slide 6: NET FIT WOULD BE IDEAL, ALTHOUGH NOT PRACTICAL (TOLERANCE STACKUP)
interference fit (common in metals) causes high shearing forces on reinforcing fibers and bends them down -> breaking the matrix resin, a 0.0007 inch interference reported to result in damage (see fig. 7a and b, pg. 708, ASM Vol. 1)
composite fibers can accommodate much more compression -> a controlled expansion of a sleeve that remains statically in contact with the fibers is successful and can produce interferences up to 0.006 inches (see fig. 7c and d, pg. 708, ASM Vol. 1)
although all that is desired is a "net" fit, the interference is used to absorb the tolerances on the hole and fastener

## Slide 7: ADVANTAGES OF NET/INTERFERENCE FIT
less joint deflection
equal fastener load sharing
reduction of relative fastener flexibility that causes localized high bearing stresses
reduction or delay in hole growth/degradation
lightning strike protection
  if lightning strike (up to 100,000 A for 0.050 s. max dwell time) attaches to a fastener, the current must be dissipated through the fibers perpendicular to the fastener hole (carbon fibers 1,000 times more resistive than Al and epoxy resin 1,000,000 times)
  current must be dissipated in short period of time to minimize damage

## Slide 8: POTENTIAL FOR GALVANIC CORROSION NEEDS TO BE CONSIDERED
cannot use gr/ep with (less noble metals) Al and alloy steel (non-corrosion resistant) – see https://www.corrosionpedia.com/galvanic-corrosion-of-metals-connected-to-carbon-fiber-reinforced-polymers/2/1556
with gr/ep use Ti, CRES, Inconel
Ti cannot be used in contact with Al

## Slide 9: FASTENER DESIGN GUIDE (major aerospace manufacturer)
Fastener Selection Parameters
Fastener Selection Flow Diagram
drawing callouts often reference some military specification