## Slide 1: PULTRUSION

## Slide 2: PULTRUSION PROCESS
automated process for manufacturing composite materials into continuous cross-section profiles

## Slide 3: PULTRUSION APPLICATIONS
usually grouped into two categories
  solid rod and bar stock
  structural profiles
selection of pultruded parts not strictly based on price competitiveness, but other characteristics not found in traditional materials
  non-conductive ladder rails (highest volume application)
  applications in the electric utility industry (insulating properties)
    insulators
    hot-line maintenance tools
    booms for electrical bucket trucks
  grating systems (walkways, stairs, ...) in highly corrosive environments

## Slide 4: REINFORCEMENTS USED IN PULTRUSION
type
  E-glass, S-glass
  carbon/graphite
  aramid
form
  roving
  mat
  fabric

## Slide 5: RESINS USED IN PULTRUSION
low viscosities (500 cps)
ability to cure quickly
polyester (most common)
  control of styrene level critical - must achieve satisfactory cross-link structure without leaving residual (unreacted) styrene in finished composite
  shrinks upon cure facilitating release from die
vinyl ester resin
  slower process speed due to slower reaction
epoxy
  very slow process speed
  reaction rate is very slow - gelation of epoxy resins occurs at a later stage of reaction - critical exotherm must be contained within die
  typically shorter pot life
  drip off at die entrance must be discarded rather than recirculated to bath
  temp profiles typically hotter
  tendency to bond strongly to die wall

## Slide 6: SIX KEY ELEMENTS IN PULTRUSION PROCESS
three occur prior to pultruder
  reinforcement handling system (creel)
  resin impregnation station
  material forming area
three integral to pultruder
  components that heat and consolidate
  equipment to pull pultrusion
  equipment to cut pultrusion

## Slide 7: REINFORCEMENT HANDLING SYSTEM
continuous fiber (roving) creels usually first station on a process line
directly followed by creels designed for rolls of mat, fabric, and/or veil
as material travels toward impregnation area, alignment must be controlled - accomplished by using creel cards that have predefined specific locations for each material

## Slide 8: RESIN IMPREGNATION
dip bath (most common)
  fibers passed over and under wet-out bars, causing fiber bundles to spread and accept resin
  suitable for products that are all roving construction or that are easily formed from resulting flat ply that exits wet-out bath
custom resin baths
  when impractical to dip materials into bath (i.e. vertical mat)
  bath walls and plates are machined and positioned to accommodate necessary preform shape and alignment
  impregnate without moving reinforcements outside of their intended forming path

## Slide 9: FORMING FOLLOWS IMPREGNATION
forming guides attached in front of pultrusion die
ensure positive alignment of the formed materials with the die cavity
sizing of forming guide slots, holes, and clearances must be designed to prevent excess tension on relatively weak and wet materials, yet allow sufficient resin removal to prevent high force at die entrance
forming guide materials include Teflon, polyethylene, chromium plated steel and various sheet steel alloys
requires experienced craftsperson to design and fabricate forming guides
hollow parts use mandrel cantilevered through pultrusion die

## Slide 10: ALTERNATIVE IMPREGNATING AND FORMING METHOD
inject resin directly into die after dry materials formed
eliminates problems associated with dip bath limitations
  satisfactory wet-out
  air entrapment
  maximum fiber content
  environmental concerns with (covered) dip bath

## Slide 11: CONSOLIDATING AND CURING
positioning and anchoring of die - must transfer thrust that develops as material is pulled through die to the frame without allowing movement of die or deflection of frame
source of cooling water or air is essential in front of die at start-up and during temporary shutdown periods to prevent premature gelation at die entrance
heating of die
  electric
  circulating thermal fluid
  others (microwave, rf)

## Slide 12: THREE COMMON CURING METHODS
die curing
  most often multiple zones
  start at low temp and increase across zones
  easy to control and achieve steady state
tunnel oven method
  pultrusion is gelled in die and fully cured during travel through oven
  length of oven determined by line speed, part dimensions, and curing characteristics of resins
split die method
  split mold halves brought up against pultrusion as it exits die
  line stops while curing takes place, continues when curing complete
  non-uniform cross-section possible

## Slide 13: MOST CRITICAL PULTRUSION PROCESS CONTROL PARAMETER IS DIE HEATING PROFILE
determines rate of reaction
position of reaction within die
magnitude of peak exotherm
improperly cured pultrusion will exhibit poor physical and mechanical properties, yet may visually appear identical to adequately cured pultrusion

## Slide 14: CLAMPING AND PULLING
10 ft or more between die exit and pulling device to allow hot pultrusion to cool and develop adequate strength to resist clamping forces
intermittent-pull reciprocating clamp
  single clamp
  clamp - pull - release - return
  during return interval, pultrusion remains stationary until clamping and pulling cycle can be reinitiated
continuous-pull reciprocating clamp (most common)
  clamp - pull - release return cycle is synchronized between two pullers to provide continuous pulling motion
continuous-belt pullers
  double continuous belts through which the pultrusion is passed
  contact area of belted puller is generally longer than found with reciprocating clamp pullers - less pressure applied to profile

## Slide 15: CUTOFF
radial arm saw or pivot saw on table that moves downstream with product flow
continuous-grit carbide or diamond edge blade

## Slide 16: ADVANTAGES OF PULTRUSION
high throughput rate
  “finished part”
  lines can reportedly produce certain profiles at 10 - 15 ft/min
  more typical line speeds in the range of 2 - 4 ft/min
high material usage (low process waste, part is “net”)
able to use wide variety of reinforcement types, forms and styles with many thermosetting resins and fillers
complex thin-walled shapes can be fabricated (traditionally extruded in aluminum, PVC)
can fabricate extremely large parts
can fabricate any transportable length parts

## Slide 17: DISADVANTAGES OF PULTRUSION
cross-sections typically need to be constant
difficult to maintain tight tolerances
  shrinkage (commonly 2% - 3%)
    difficult to control
    cross-section dependent (variation in thickness)
  straightness along length
    lateral and bowing
    may be able to “remove” with force
quick curing resin systems typically have lower mechanical properties
complexity of process
  problems resulting from resin and fibers accumulating and building up at die entrance
  parts are run resin rich to account for fiber anomalies, strength is sacrificed
  voids may result in parts if excessive opening given at die entrance