## Slide 1: SANDWICH COMPOSITES

## Slide 2: COMPONENTS OF SANDWICH COMPOSITES
face sheets, facings, skins
core material
adhesive

## Slide 3: FACE SHEETS
traditional composite materials

## Slide 4: CORE MATERIALS
honeycomb (Hexcel, Plascore)
  method of manufacture
    expansion process or corrugation process (see mfg processes)
    determines difference in L/W performance (see data sheet)
  materials (see property comparison)
    aluminum (CR-PAA/CRIII 5052 and 5056, ACG)
    aramid fiber reinforced phenolic (HRH-10 (Nomex), KOREX)
    glass reinforced phenolic (HRP, HFT)
    glass reinforced polyimide (HRH-327)
    thermoplastic
closed cell rigid foam
  Rohacell (polymethacrylimide)
  Divinycell, CoreLite (polyvinyl chloride)
cast (two-part expanding) foam
balsa (Baltek, CoreLite)

## Slide 5: ADHESIVE BONDING
rely on resin used in face sheet (particularly in wet lay-up)
film adhesive
select adhesive according to application

## Slide 6: FABRICATION PROCESS
forming
  machining
  for foams
    curing/annealing to achieve desired density and strength
    thermoforming
cleaning
  vacuuming
  for aluminum - vapor degreasing
  for Nomex - ethyl alcohol
drying (elevated temperature in air-circulating oven)
face sheets cocured or post-bonded
must check compaction pressure will not crush core materials or cause intercell buckling of face sheets

## Slide 7: ADDITIONAL CONSIDERATIONS
hardpoints for fasteners
edge closures